ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC011 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | June 17, 1999 |  |
| Date of final welding | June 22, 1999 |  |
| Date of surface protection | January 20, 2000 |  |
| Coil identification: masters | Pallet #87 |  |
| Box identification: spacers | Shipment 1 |  |
| Glue batch number | Hardener 20335283 Resin 20356883 |  |
| Glue drop size – start (gm) | 0.1692 |  |
| Glue drop size – middle (gm) | 0.1734 |  |
| Glue drop size – end (gm) | N/A |  |
| Stacking time (h: m) | 3:10 |  |
| Gluing curing time ( h: m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Mark Cosentino | Ideal Tool |
| Final Welding: Welder name | Mark Cosentino | Ideal Tool |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: N/A

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC011 | Institute: University of Chicago |
| --- | --- |

THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.89 | 291.19 | 291.24 | 291.26 | 291.24 | 291.23 | 291.13 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.64 | 291.02 | 291.16 | 291.18 | 291.18 | 291.21 | 291.20 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.82 | 290.72 | 291.11 | 291.12 | 291.16 | 291.17 |

Maximum deviation from nominal (+): N/A

Maximum deviation from nominal (-): 1.06; 290.64

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC011 | Institute: University of Chicago |
| --- | --- |

SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20356883					Hardener identification: 20335283

Dosage control (gm/point). (Final range to be determined from glue system qualification)

Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1692 |  |  |  |  | 0.1692 |
| Post-Stacking (gm/point) | 0.1692 | 0.1734 |  |  |  | 0.1713 |

Pre-Cleanout Inspection

Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 4 | 0 | 2 | 0 | 0 | 0 | 0 | 0 | 2 | 0 | 15 |

Post-Cleanout Inspection

Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean(OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Alexis Mills/ Matt Fillo Date: January 24, 2000 Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC011 | Institute: University of Chicago |
| --- | --- |

FINAL WELDING

Date of Welding: June 22, 1999

Welding Filler Rod Material: ER70S-2

Weld Inspection (as defined in technical specification) – OK/NOK: OK

1.	Inspection commenced before weld cooled to ambient temperature

(within 20 minutes)

2.	No Cracks

3.	Thorough fusion

4.	All craters filled to full cross section

5.	Undercut does not exceed .25mm

6.	No visible porosity

7.	Weld profile conformance

Note any required repairs:

Note any variances from technical specification:

Comments:

Welder Name (Print): Mark Cosentino Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC011 | Institute: University of Chicago |
| --- | --- |

SURFACE PROTECTION

Date of Surface protection: January 20, 2000

Paint batch and production date:

Batch Number: 0199 20

Production Date: 14VIL 1999

Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 20 |

Control of Paint Flow

Energy velocity, as specified in general QC procedures note.

Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm |  |  |  |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 30minutes

Y= 5.7083333 cm/minutes  5.709 cm/minute

Z= 1.051 minutes  63.06 seconds

Visual Inspection (OK/NOK): OK

Comments:

Mixed paint to 20 sec.  Start to fill hopper at 14:15 at 40 PSI.  The submodule was inserted at 1445 and totally submerged 1500.  Started to empty the hopper at 1530 at 40 PSI and finished at 1600.  The submodule was horizontal at 1630.

Quality Control Technician (Print):Greg Wilkins Date: Signature: