ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC012 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | June 21, 1999 |  |
| Date of final welding | July 8, 1999 |  |
| Date of surface protection | May 25, 2000 | Greg Wilkins |
| Coil identification: masters | Pallet #87 (27), #2 (5) |  |
| Box identification: spacers | 5-1/13 |  |
| Glue batch number | Hardener 20335283 Resin 20356883 |  |
| Glue drop size – start (gm) | 1.572 |  |
| Glue drop size – middle (gm) | N/A |  |
| Glue drop size – end (gm) | N/A | Finished gluing by hand |
| Stacking time (h: m) | 3:50 |  |
| Gluing curing time ( h: m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Mark Cosentino | Ideal Tool |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: N/A

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC012 | Institute: University of Chicago |
| --- | --- |

THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.52 | 291.03 | 291.13 | 291.06 | 290.95 | 290.97 | 290.83 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.37 | 290.76 | 290.89 | 290.88 | 291.02 | 291.02 | 290.79 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.40 | 290.60 | 290.80 | 290.83 | 290.80 | 290.82 |

Maximum deviation from nominal (+): N/A

Maximum deviation from nominal (-): 1.33; 290.37

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC012 | Institute: University of Chicago |
| --- | --- |

SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20356883				Hardener identification: 20335283

Dosage control (gm/point). (Final range to be determined from glue system qualification)

Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1572 |  |  |  |  | 0.1572 |
| Post-Stacking (gm/point) | 0.1572 |  |  |  |  | 0.1572 |

Pre-Cleanout Inspection

Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 1 | 0 | 1 | 0 | 1 | 0 | 2 | 0 | 1 | 0 | 12 |

Post-Cleanout Inspection

Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC012 | Institute: University of Chicago |
| --- | --- |

FINAL WELDING

Date of Welding: July 8, 1999

Welding Filler Rod Material: ER70S-2

Weld Inspection (as defined in technical specification) – OK/NOK: OK

1.	Inspection commenced before weld cooled to ambient temperature

(within 20 minutes)

2.	No Cracks

3.	Thorough fusion

4.	All craters filled to full cross section

5.	Undercut does not exceed .25mm

6.	No visible porosity

7.	Weld profile conformance

Note any required repairs:

Final welds were insufficient.  Cindy Dyrda welded another pass to specifications.

Note any variances from technical specification:

Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC012 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: May 25, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14VIL1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 14 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 20 minutes

Y= 8.5625

Z= 0.7007  42.04 seconds/ 6 cm

- Visual Inspection (OK/NOK): OK

- Comments:

- Started to fill the hopper at 09:15 at 40 PSI.  The submodule was inserted at 09: 35 and was totally submerged at 09:40.  Emptying procedures were started at 10:10 at 40 PSI and finished at 10:30.  It was horizontal at 11:00

Quality Control Technician (Print): Greg Wilkins Date: Signature: