ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | July 12, 1999 |  |
| Date of final welding | N/A | Possibly the 13th of July |
| Date of surface protection | May1, 2000 | Greg Wilkins |
| Coil identification: masters | Pallet #82 |  |
| Box identification: spacers | 11-9/13 |  |
| Glue batch number | Hardener 20335283 Resin 20356883 |  |
| Glue drop size – start (gm) | 1.905 |  |
| Glue drop size – middle (gm) | 1.980 |  |
| Glue drop size – end (gm) | 1.958 |  |
| Stacking time (h: m) | 3:20 |  |
| Gluing curing time ( h: m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Mark Cosentino | Ideal Tool |
| Final Welding: Welder name | N/A |  |
| Weld inspection (OK/NOK) | OK |  |
| Observations: Top keys #13 added after stack. Cut weld bars on July 14, 1999 and added the key to #13 and recompressed on July 14, 19999. |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.31 | 291.36 | 291.47 | 291.30 | 290.95 | 290.98 | 291.58 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.27 | 291.46 | 291.42 | 291.36 | 291.04 | 291.03 | 291.70 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.37 | 291.33 | 291.34 | 291.15 | 290.85 | 290.80 |

Maximum deviation from nominal (+): N/A

Maximum deviation from nominal (-): 0.90; 290.80

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | N/A | N/A |
| --- | --- | --- |
| 5.75” | N/A | N/A |
| Bottom | N/A | N/A |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | N/A | N/A |
| --- | --- | --- |
| 5.75” | N/A | N/A |
| Bottom | N/A | N/A |

* 5.75” refers to 5.75” from bottom

Observations:

The feeler gauge measurements were not taken for this submodule.

Quality Control Technician (Print): N/A Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20356883			 Hardener identification: 20335283

Dosage control (gm/point). (Final range to be determined from glue system qualification)

Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1905 |  |  |  |  | 0.1905 |
| Post-Stacking (gm/point) | 0.1905 | 0.1980 | 0.1958 |  |  | 0.1948 |

Pre-Cleanout Inspection

Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 3 | 0 | 0 | 0 | 2 | 0 | 0 | 1 | 2 | 1 | 0 |

Post-Cleanout Inspection

Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK):OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

FINAL WELDING

Date of Welding: N/A

Welding Filler Rod Material: ER70S-2

Weld Inspection (as defined in technical specification) – OK/NOK: OK

1.	Inspection commenced before weld cooled to ambient temperature

(within 20 minutes)

2.	No Cracks

3.	Thorough fusion

4.	All craters filled to full cross section

5.	Undercut does not exceed .25mm

6.	No visible porosity

7.	Weld profile conformance

Note any required repairs:

Note any variances from technical specification:

Comments:

No changes have yet been made to the welding procedure of the ATLAS project.

Welder Name (Print): N/A Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC016 | Institute: University of Chicago |
| --- | --- |

SURFACE PROTECTION

- Date of Surface protection: May 1, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Date: 14Vil1999

Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 14 |

Control of Paint Flow

Energy velocity, as specified in general QC procedures note.

Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec./6cm | 42.04 sec./6cm | 42.04 sec./6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 20

Y= 8.5625

Z= 0.7707  42.04 seconds

Visual Inspection (OK/NOK): OK

Comments:

Started to fill the hopper at 13:10 at 40 PSI. The submodule was inserted at 13:40 and was totally submerged at 13:45.  Started emptying procedures at 14:10 and 40 PSI.  The hopper was completely empty at 14:30 and the submodule was then laid horizontal at 13:55.

Quality Control Technician (Print): Greg Wilkins Date: Signature: