ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC017 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | July 13, 1999 |  |
| Date of final welding | N/A |  |
| Date of surface protection | March 9, 2000 |  |
| Coil identification: masters | Pallet #82 |  |
| Box identification: spacers | 11-9/13 |  |
| Glue batch number | Hardener 20335283 Resin 20356883 |  |
| Glue drop size – start (gm) | 1.863 |  |
| Glue drop size – middle (gm) | 1.980 |  |
| Glue drop size – end (gm) | N/A |  |
| Stacking time (h: m) | 3:15 |  |
| Gluing curing time ( h: m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Mark Cosentino | Ideal Tool |
| Final Welding: Welder name | Mark Cosentino | Ideal Tool |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: N/A

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC017 | Institute: University of Chicago |
| --- | --- |

THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.07 | 291.16 | 291.34 | 291.30 | 291.25 | 291.09 | 290.35 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.85 | 291.23 | 291.23 | 291.27 | 291.28 (291.24) | 291.20 | 290.76 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.01 | 291.11 | 291.19 | 291.28 | 291.22 | 291.13 |

Maximum deviation from nominal (+): N/A

Maximum deviation from nominal (-): 1.35; 290.35

Quality Control Technician (Print): Marva Maya Date: March 16, 2000 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC017 | Institute: University of Chicago |
| --- | --- |

SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20392483			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | .1863 |  |  |  |  | .1863 |
| Post-Stacking (gm/point) | .1863 | .1980 |  |  |  | .1921 |

Pre-Cleanout Inspection

Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 14 | 2 | 0 | 1 | 3 | 8 | 2 | 1 | 0 | 1 | 15 |

Post-Cleanout Inspection

Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC017 | Institute: University of Chicago |
| --- | --- |

FINAL WELDING

Date of Welding: N/A

Welding Filler Rod Material: ER70S-2

Weld Inspection (as defined in technical specification) – OK/NOK: OK

1.	Inspection commenced before weld cooled to ambient temperature

(within 20 minutes)

2.	No Cracks

3.	Thorough fusion

4.	All craters filled to full cross section

5.	Undercut does not exceed .25mm

6.	No visible porosity

7.	Weld profile conformance

Note any required repairs:

Note any variances from technical specification:

Comments:

Welder Name (Print): Mark Cosentino Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC017 | Institute: University of Chicago |
| --- | --- |

SURFACE PROTECTION

Date of Surface protection: March 9, 2000

Paint batch and production date:

Batch Number: 0199 20

Production Date: 14Vil 1999

Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 19 |

Control of Paint Flow

Energy velocity, as specified in general QC procedures note.

Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 63.07sec/6cm | 63.07sec/6cm | 63.07sec/6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 30 minutes

Y= 5.708333

Z= 0.951  63.07 seconds

Visual Inspection (OK/NOK): OK

Comments:

Started to fill the hopper at 15:55 at 40 PSI and then inserted submodule #017 at 16:25.  It was totally submerged at 16:30.  Started to empty the hopper at17:00 at 40 PSI and finished emptying at 17:30. The submodule was finally horizontal at 18:00.

Quality Control Technician (Print): Greg Wilkins Date: Signature: