ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC020 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL |  | ### Data |  | ### Comments |
| --- | --- | --- | --- | --- |
| #### Date of the stacking |  | July 16, 1999 |  |  |
| Date of final welding |  | N/A |  |  |
| Date of surface protection |  | March 29, 2000 |  | Greg Wilkins |
| Coil identification: masters |  | Pallet #40 |  |  |
| Box identification: spacers |  | 11-9/13 |  |  |
| Glue batch number |  | Hardener 20405183 Resin 20392483 |  |  |
| Glue drop size – start (gm) |  | 0.1495 |  |  |
| Glue drop size – middle (gm) |  | 0.15715 |  |  |
| Glue drop size – end (gm) |  | 0.1535 |  |  |
| Stacking time (h:m) |  | 3:20 |  |  |
| Gluing curing time ( h:m) |  | N/A |  |  |
| Glue hardness (OK/NOK) |  | OK |  |  |
| Glue clean out (OK/NOK) |  | OK |  |  |
| Tack welding: Welder name |  | Mark Cosentino |  | Ideal Tools |
| Final Welding: Welder name |  | Cindy Dyrda |  | UCEC |
| Weld inspection (OK/NOK) |  | OK |  |  |
| Observations: |  |  |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC020 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 (290.61) | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.89 | 290.86 | 290.98 | 290.89 | 290.70 | 290.56 | 290.46 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.01 | 291.11 | 291.13 | 291.04 | 290.90 | 290.82 | 290.39 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.02 | 290.84 | 291.05 | 290.96 | 290.82 | 290.70 |

- Maximum deviation from nominal (+): N/A

- Maximum deviation from nominal (-): 290.39; 1.31

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC020 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20392483			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | .1495 |  |  |  |  | .1495 |
| Post-Stacking (gm/point) | .1495 | .1515 | .1535 |  |  | .1515 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 2 | 0 | 0 | 1 | 0 | 0 | 0 | 1 | 0 | 0 | 10 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC020 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: N/A

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC020 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: March 29, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Date: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 18 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 63.07 sec/ 6cm | 63.07 sec/ 6cm | 63.07 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z seconds

X= 30

Y= 5.708333

Z=1.051  63.07 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Started to fill the hopper at 1300 at 40 PSI.  The submodule was inserted at 13:35 and was totally submerged at 13:45.  The emptying procedures were started at 14:25 at 40 PSI and finished at 14:55.  The submodule was horizontal at 15:30.

Quality Control Technician (Print): Greg Wilkins Date: Signature: