ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC023 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | July 21, 1999 |  |
| Date of final welding | N/A | Possibly the 27th of July |
| Date of surface protection | January 28, 2000 |  |
| Coil identification: masters | Pallet #33 |  |
| Box identification: spacers | 11-9/13 (8) 11-8/13 (4) |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | 1.473 |  |
| Glue drop size – middle (gm) | 1.542 |  |
| Glue drop size – end (gm) | 1.495 |  |
| Stacking time (h:m) | 3:00 |  |
| Gluing curing time ( h:m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dydra | Ideal Tool |
| Final Welding: Welder name | Cindy Dydra | Ideal Tool |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC023 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.69 | 290.97 | 291.05 | 290.93 | 290.91 | 290.70 | 290.25 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.57 | 290.68 | 290.95 | 290.91 | 290.85 | 290.76 | 290.46 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.69 | 290.86 | 290.77 | 290.90 | 290.83 | 290.72 |

- Maximum deviation from nominal (+): N/A

- Maximum deviation from nominal (-): 290.25; 1.45

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC023 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Glueing

Resin identification: 20392483 			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | .1473 |  |  |  |  | .1473 |
| Post-Stacking (gm/point) | .1473 | .1542 | .1495 |  |  | .1503 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 3 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC023 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: N/A. Possibly the 27th of July

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC023 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: January 28, 2000

- Paint batch and production date:

Batch Number: 0199 20

# Production Date: 14Vil 1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 20 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 63.07 sec/6 cm | 63.07 sec/6 cm | 63.07 sec/6 cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 30 minutes

Y= 5.708 cm

Z= 1.05 minutes  63.07 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed paint at 20 sec.  Started to fill hopper at 12:25 at 40 PSI and inserted submodule at 13:00 and totally submerged at 13:10.  Started to empty the hopper at 13:40 at 40 PSI and done at 14:10.  The submodule was horizontal at 14:45.

Quality Control Technician (Print): Greg Wilkins Date: Signature: