ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC031 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | August 3, 1999 |  |
| Date of final welding | August 10, 1999 |  |
| Date of surface protection | May 9, 2000 |  |
| Coil identification: masters | Pallet #06 |  |
| Box identification: spacers | 15-2/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | 3:05 |  |
| Glue drop size – middle (gm) | 1.715 |  |
| Glue drop size – end (gm) | 1.698 |  |
| Stacking time (h:m) | 1.720 |  |
| Gluing curing time ( h:m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dydra | August 4, 1999 |
| Final Welding: Welder name | Cindy Dydra | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC031 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.99 | 291.03 | 291.43 | 291.23 | 291.15 | 291.03 | 290.64 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.94 | 291.08 | 291.18 | 291.05 | 290.96 | 290.83 | 290.67 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 290.92 | 291.02 | 291.25 | 291.11 | 291.01 | 290.93 |

- Maximum deviation from nominal (+): N/A

- Maximum deviation from nominal (-): 290.64; 1.06

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC031 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20392483 			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1715 |  |  |  |  | 0.1715 |
| Post-Stacking (gm/point) | 0.1715 | 0.1698 | 0.1720 |  |  | 0.1711 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 16 | 0 | 0 | 1 | 0 | 0 | 1 | 0 | 2 | 0 | 0 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC031 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: August 10, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC031 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: May 9, 2000

- Paint batch and production date:

Batch number: 0199 20

Production Date: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 14 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/6cm | 42.04 sec/6cm | 42.04 sec/6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 20 minutes

Y= 8.5625

Z= 0.7007  42.04 sec/ 6cm

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed the paint to 14 seconds and added one can of paint to the barrel mix to 14seconds.  Started to fill the hopper at 09:45 at 40 PSI. The submodule was inserted at 10:05 and totally submerged at 10:10.  Emptying procedures were started at 10:35 at 40PSI and finished at 10:55.  The submodule was horizontal at 11:20.

Quality Control Technician (Print): Greg Wilkins Date: Signature: