ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | September 17, 1999 |  |
| Date of final welding | October 6th |  |
| Date of surface protection | February 25, 2000 | Last painted on February 29, 2000 |
| Coil identification: masters | Pallet # 61 |  |
| Box identification: spacers | 11-6/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | .1687 | Taken at 11:10 |
| Glue drop size – middle (gm) | .1662 | Taken at 13:35 |
| Glue drop size – end (gm) | .1651 | Taken at 14:00 |
| Stacking time (h:m) | 2:50 |  |
| Gluing curing time ( h:m) | N/A |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | September 20, 1999 |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: No shim. Feeler gauge measurements are high in 2 places (11-19-99). |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.70 | 291.86 | 291.82 | 291.78 | 291.61 | 291.42 | 290.89 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.58 | 291.72 | 291.65 | 291.64 | 291.46 | 291.22 | 291.05 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.68 | 291.75 | 291.75 | 291.68 | 291.49 | 291.30 |

- Maximum deviation from nominal (+): 291.86; 0.16

- Maximum deviation from nominal (-): 290.89; 0.81

Quality Control Technician (Print): Marva Maya Date: November 19, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0.00 | 0.014* |
| --- | --- | --- |
| 5.75” | 0.006 | 0.006 |
| Bottom | 0.006 | 0.00 |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | 0.00 | 0.012* |
| --- | --- | --- |
| 5.75” | 0.006 | 0.007 |
| Bottom | 0.006 | 0.003 |

* 5.75” refers to 5.75” from bottom

Drawings and Observation/Notes:

High at both section 1 and narrow end right side.

Quality Control Technician (Print): Marva Maya Date: November 19, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 	20392483		 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | .1666 |  |  |  |  | .1666 |
| Post-Stacking (gm/point) | .1666 | .1673 | .1686 |  |  | .1675 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 9 | 0 | 0 | 0 | 1 | 1 | 3 | 1 | 1 | 0 | 9 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: October 6, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

(3” root pass on center at joint, cooled, completed.)

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC053 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: February 25, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 18 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 63.07 sec/ 6cm | 63.07 sec/ 6cm | 63.07 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 30

Y= 5.70833

Z= 0.951  63.07 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Started to fill the hopper at 14:30 and inserted submodule 53 at 15:30.  It was totally submerged at 15:35.  Started emptying procedure at 16:10 at 40 PSI and completed at 16:40.  The submodule was then horizontal at 17:15.

Quality Control Technician (Print): Greg Wilkins Date: Signature: