ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC055 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL |  | ### Data |  | ### Comments |
| --- | --- | --- | --- | --- |
| #### Date of the stacking |  | September 22, 1999 |  |  |
| Date of final welding |  | October 1, 1999 |  |  |
| Date of surface protection |  | June 16, 2000 |  |  |
| Coil identification: masters |  | Pallet # 18 |  | Opened September 13, 1999 |
| Box identification: spacers |  | 11-6/13 |  | Opened September 13, 1999 |
| Glue batch number |  | Hardener 20405183 Resin 20392483 |  |  |
| Glue drop size – start (gm) |  | .1661 |  | Started at 9:55 am |
| Glue drop size – middle (gm) |  | .1691 |  | Taken at 11:25 am |
| Glue drop size – end (gm) |  | .1615 |  | Taken at 12:55 pm |
| Stacking time (h:m) |  | 3:0 |  |  |
| Gluing curing time ( h:m) |  | N/A |  |  |
| Glue hardness (OK/NOK) |  | OK |  |  |
| Glue clean out (OK/NOK) |  | OK |  |  |
| Tack welding: Welder name |  | Cindy Dydra |  | UCEC |
| Final Welding: Welder name |  | Cindy Dyrda |  | UCEC |
| Weld inspection (OK/NOK) |  | OK |  |  |
| Observations: | No shim |  |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC055 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.79 | 291.84 | 291.82 | 291.69 | 291.46 | 291.18 | 290.57 |

| Point | 14 | 13* | 12* | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.89 | 292.18 | 292.01 | 291.94 | 291.76 | 291.63 | 290.98 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.85 | 291.97 | 291.85 | 291.74 | 291.56 | 291.37 |

*The submodule is to high in marked areas

- Maximum deviation from nominal (+): 292.18; 0.48

- Maximum deviation from nominal (-): 290.57; 1.13

Quality Control Technician (Print): Mathew Fillo Date: October 15, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0 | 0.002 |
| --- | --- | --- |
| 5.75” | 0.007 | 0.004 |
| Bottom | 0.0015 | 0 |

- Section 1:

- (.5” from weld area on narrow end)

- Narrow end			Wide end

- Left Side:				Right Side:

| Top | 0.005 | 0.004 |
| --- | --- | --- |
| 5.75” | 0.007 | 0.004 |
| Bottom | 0 | 0 |

* 5.75” refers to 5.75” from bottom

Observations:

Quality Control Technician (Print): Mathew Fillo Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC055 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 	20392483		 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1661 |  |  |  |  | 0.1661 |
| Post-Stacking (gm/point) | 0.1661 | 0.1691 | 0.1615 |  |  | 0.1656 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | All 1Pin drop | 0 | 0 | 0 | 0 | 4 | 0 pin down | 1 | 1 | 0 | 1 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC055 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: October 1, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

3” Shrinkage control weld:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC055 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: June 16, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 15 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 seconds/ 6cm | 42.04 seconds/ 6cm | 42.04 seconds/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 20

Y= 8.5625

Z= 0.7007 42.04 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed the old paint to 14 seconds and the new can of paint opened to 15 seconds and added it to the paint drum.  Started to fill the hopper at 12:50 at 40 PSI.  Submodule 055 was inserted at 13:30 and was totally submerged at13:35. The emptying procedures were started at 14:00 at 40 PSI and finished at 14:20.  The submodule was horizontalat15: 10.

Quality Control Technician (Print): Greg Wilkins Date: Signature: