ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | October 15, 1999 | Greg and Matt |
| Date of final welding | October 25, 1999 |  |
| Date of surface protection | October 7, 1999 |  |
| Coil identification: masters | Pallet #18 |  |
| Box identification: spacers | 11-6/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | .16376 | Taken at 10:15 |
| Glue drop size – middle (gm) | .16394 | Taken at 12:17 |
| Glue drop size – end (gm) | .1503 | Taken at 13:50 |
| Stacking time (h:m) | 3:20 |  |
| Gluing curing time ( h:m) | 21:40 | Released at 11:40 on 10/16/99 |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | UCEC. On 10/18/99 |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: Started .007” shim but no shim on top of submodule. Area7- 7th spacer wrong. |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.74 | 291.97 | 292.00 |  | 291.89 | 291.68 | 291.10 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.76 | 291.83 | 291.84 | 291.79 | 291.57 | 291.37 | 291.05 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.74 | 291.86 | 291.97 | 291.85 | 291.66 | 291.46 |

- Maximum deviation from nominal (+): 292.00; 0.3

- Maximum deviation from nominal (-): 291.05; 0.65

Quality Control Technician (Print):Elizabeth Pod, Cliff McLue Date: October 26, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0.005 | 0.003 |
| --- | --- | --- |
| 5.75” | 0.005 | 0.005 |
| Bottom | 0.0 | 0.005 |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | 0.007 | 0.002 |
| --- | --- | --- |
| 5.75” | 0.005 | 0.002 |
| Bottom | 0.003 | 0.002 |

* 5.75” refers to 5.75” from bottom

Drawings and Observation/Notes:

Wide end was also taken:

- Left Side:				Right Side:

| Top | 0.004 | 0.005 |
| --- | --- | --- |
| 5.75” | 0.004 | 0.005 |
| Bottom | 0.003 | 0.0 |

Quality Control Technician (Print): Elizabeth Pod, Cliff McLue Date: October 26, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 	20392483		 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.16376 |  |  |  |  | 0.1638 |
| Post-Stacking (gm/point) | 0.16376 | 0.16394 | 0.1503 |  |  | 0.1594 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 12 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1 | 8 |

Observation:  No pins dropped.

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: October 25, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

(3”root pass on center, coole, completed.)

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

- Comments:

3” root pass on center, cooled, completed.

Welder Name (Print):Cindy Dyrda Date: 10-25-99 Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC057 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: June 16, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 14-15 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 seconds/ 6cm | 42.04 seconds/ 6cm | 42.04 seconds/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 20

Y= 8.5625

Z= 0.7007  42.04 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed the old paint to 14 seconds and then opened a new can of paint and mixed it to 15 seconds and then added it to the paint drum.  Started to fill at 14:30 at 40 PSI and then inserted submodule 057at 14:50and it was totally submerged at 15:00.  Started emptying procedures at 15:40 at 40 PSI and finished at 16:00. The submodule was horizontal at 16:30.

Quality Control Technician (Print): Greg Wilkins Date: Signature: