ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC061 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | October 29, 1999 | Elizabeth, Matt, Greg, Lex, Tom |
| Date of final welding | November 15, 1999 |  |
| Date of surface protection | June 22, 2000 | Greg/Darren |
| Coil identification: masters | Pallet #27 |  |
| Box identification: spacers | 11-6/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | 1.632 | Taken: 11:40 |
| Glue drop size – middle (gm) | 1.676 | Taken: 13:10 |
| Glue drop size – end (gm) | 1.643 | Taken: 14:35 |
| Stacking time (h:m) | 3:35 |  |
| Gluing curing time ( h:m) | 21:05 | Unclamped 11:00 on 11/01/99 |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | On 11/01/99. UCEC. |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: | 0.15” =.40mm Shim on middle section. |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC061 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.48 | 291.45 | 291.40 | 291.38 | 291.72 | 291.53 | 291.20 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.46 | 291.58 | 291.45 | 291.42 | 291.79 | 291.67 | 291.20 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.45 | 291.53 | 291.45 | 291.43 | 291.72 | 291.53 |

- Maximum deviation from nominal (+): 291.72; 0.02

- Maximum deviation from nominal (-): 291.20; 0.5

Quality Control Technician (Print): Cliff McLue Date: November 16, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC061 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20392483		 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1632 |  |  |  |  | 0.1632 |
| Post-Stacking (gm/point) | 0.1632 | 0.1676 | 0.1643 |  |  | 0.1650 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

Taken: 11-03-99

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | ALL | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC061 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: November 15, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

Narrow end was welded 3” every 6” on center.  Cooled until barely warm to the touch.  Repeated until complete.  All welds on narrow end were done in this manner.

- Comments:

Welder Name (Print): Cindy Dyrda Date: November 15, 1999 Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC061 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: June 22, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 15 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 20

Y= 8.5625

Z= 0.7007 42.04 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed paint to 15 seconds.  Started to fill the hopper at 12:30 at 40 PSI.  The submodule was inserted at 13:00 and finally submerged at 13:05.  The emptying procedures were started at 13:30 at 40 PSI and finished and 13:50. The submodule was horizontal at 14:20.

Quality Control Technician (Print): Greg Wilkins Date: Signature: