ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL |  | ### Data |  | ### Comments |
| --- | --- | --- | --- | --- |
| #### Date of the stacking |  | November 5, 1999 |  |  |
| Date of final welding |  | November 18, 1999 |  |  |
| Date of surface protection |  | May 1, 2000 |  | Greg Wilkins |
| Coil identification: masters |  | Pallet #64 |  |  |
| Box identification: spacers |  | 11/5/13 |  |  |
| Glue batch number |  | Hardener 20405183 Resin 20392483 |  |  |
| Glue drop size – start (gm) |  | .16279 |  |  |
| Glue drop size – middle (gm) |  | .15889 |  |  |
| Glue drop size – end (gm) |  | .1611 |  |  |
| Stacking time (h:m) |  | 2:55 |  |  |
| Gluing curing time ( h:m) |  | N/A |  |  |
| Glue hardness (OK/NOK) |  | OK |  |  |
| Glue clean out (OK/NOK) |  | OK |  |  |
| Tack welding: Welder name |  | Cindy Dyrda |  | UCEC |
| Final Welding: Welder name |  | Cindy Dyrda |  | UCEC |
| Weld inspection (OK/NOK) |  | OK |  |  |
| Observations: |  |  |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 5-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.50 | 291.54 | 291.52 | 291.39 | 291.69 | 291.59 | 291.36 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.56 | 291.32 | 291.50 | 291.48 | 291.60 | 291.76 | 291.36 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.61 | 291.55 | 291.56 | 291.45 | 291.64 | 291.66 |

- Maximum deviation from nominal (+): N/A

- Maximum deviation from nominal (-): 291.32; 038

Quality Control Technician (Print): Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0.003 | 0.006 |
| --- | --- | --- |
| 5.75” | 0.003 | 0.0015 |
| Bottom | 0.005 | 0.003 |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | N/A | N/A |
| --- | --- | --- |
| 5.75” | N/A | N/A |
| Bottom | N/A | N/A |

* 5.75” refers to 5.75” from bottom

Wide end:

- Left Side:				Right Side:

| Top | 0.005 | 0.002 |
| --- | --- | --- |
| 5.75” | 0.00 | 0.00 |
| Bottom | 0.005 | 0.002 |

Quality Control Technician (Print): Greg Wilkins Date: November 9, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20392483	 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | .16279 |  |  |  |  | .16279 |
| Post-Stacking (gm/point) | .16279 | .15889 | .1611 |  |  | .16093 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:			Date:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 2 | 1 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 1 | 9 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm): 	Date:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK):OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: November 18, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

Narrow end of module welded 3” on 6” center, cooled between each pass until complete.

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC063 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: May 1, 2000

- Paint batch and production date:

Batch Number: 0199 20

Production Number: 14Vil1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 14 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 52.55 sec /6cm | 52.55 sec /6cm | 52.55 sec /6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 25

Y= 6.85

Z= 0.8759 52.55 seconds

- Visual Inspection (OK/NOK): OK

- Comments:

Started to fill the hopper at 14:45 at 40 PSI. The submodule was inserted at 15:10 and was totally submerged at 15:15.  Started emptying procedures at 15:45 and 40 PSI.  The hopper was completely empty at 16:10 and the submodule was then laid horizontal at 16:35.

Quality Control Technician (Print): Greg Wilkins Date: Signature: