ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | November 17, 1999 | Marva, Matt, Tom |
| Date of final welding | December 6, 1999 |  |
| Date of surface protection | July 13, 2000 | Greg, Gabe, Tracy |
| Coil identification: masters | Pallet #21 |  |
| Box identification: spacers | 11-2/13 |  |
| Glue batch number | Hardener 20405183 Resin 20392483 |  |
| Glue drop size – start (gm) | 0.15804 |  |
| Glue drop size – middle (gm) | 0.1575 |  |
| Glue drop size – end (gm) | 0.1624 |  |
| Stacking time (h:m) | 2:55 | Done at 16:35 on 11/17/99 |
| Gluing curing time ( h:m) | 9:20 | Unclamped at 13:15 11/18/99 |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | November 18, 1999 |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 12-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Elizabeth Pod, Kelby Anderson Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.71 | 291.75 | 291.73 | 291.67 | 291.71 | 291.67 | 291.28 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.81 | 291.94 | 291.91 | 291.73 | 291.75 | 291.75 | 291.46 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.80 | 291.87 | 291.83 | 291.73 | 291.72 | 291.76 |

- Maximum deviation from nominal (+): 291.94; 0.24

- Maximum deviation from nominal (-): 291.28; 0.42

Quality Control Technician (Print): Marva Maya Date: December 16, 1999 Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0.009 | 0.0 |
| --- | --- | --- |
| 5.75” | 0.005 | 0.003 |
| Bottom | 0.0 | 0.003 |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | 0.014 | 0.003 |
| --- | --- | --- |
| 5.75” | 0.006 | 0.006 |
| Bottom | 0.004 | 0.007 |

* 5.75” refers to 5.75” from bottom

Quality Control Technician (Print): Marva Maya Date: December 16, 1999 Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20392483 			 Hardener identification: 20405183

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.15804 |  |  |  |  | 0.15804 |
| Post-Stacking (gm/point) | 0.15804 | 0.1575 | 0.1624 |  |  | 0.1593 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

Date: December 16, 1999

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 pin out | 0 | 0 | 0 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: December 6, 1999

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone. Repeated until weld is completed.

- Comments:

Welder Name (Print): Cindy Dyrda Date: December 7, 1999 Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC066 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: July 13, 2000

- Paint batch and production date:

- Batch Number: 0199 20

- Production Date: 14Vil 1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 15 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z(60) seconds

X= 20

Y= 8.5625

Z=0.7007  42.04 seconds/ 6cm

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed the paint to 15 seconds.  Started to fill the hopper at 09:45 at 40 PSI.  Inserted the submodule at 10:15 and it was totally submerged at 10:20.  Started the emptying procedure at 10:50 at 40 PSI and finished at 11:10.  The submodule was horizontal at 11:30.

Quality Control Technician (Print): Greg Wilkins Date: Signature: