ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | January 21, 2000 | Jim, Tim, Cliff, Matt, Greg, Lex, Tom |
| Date of final welding | February 8, 2000 |  |
| Date of surface protection | July 18, 2000 |  |
| Coil identification: masters | Pallet #57, #38 |  |
| Box identification: spacers | 11-3/13 |  |
| Glue batch number | Hardener 20488293 Resin 20466993 |  |
| Glue drop size – start (gm) | 0.1619 |  |
| Glue drop size – middle (gm) | 0.1634 |  |
| Glue drop size – end (gm) | 0.1638 |  |
| Stacking time (h:m) | 4:21 |  |
| Gluing curing time ( h:m) | 71:55 |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) | OK |  |
| Tack welding: Welder name | Cindy Dyrda | UCEC 01-24-00 |
| Final Welding: Welder name | Cindy Dyrda | UCEC |
| Weld inspection (OK/NOK) | OK |  |
| Observations: Shim all 0.003” |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 12-99

Last date of welder qualification (final weld)	: 7-99

Quality Control Leader: Kelby Anderson, Elizabeth Pod Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1* | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 292.09 | 291.84 | 291.73 | 291.70 | 291.48 | 291.23 | 290.87 |

| Point | 14* | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 292.08 | 291.94 | 291.75 | 291.79 | 291.56 | 291.42 | 291.11 |

| Point | 15* | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 292.11 | 291.93 | 291.71 | 291.76 | 291.53 | 291.35 |

- Maximum deviation from nominal (+): 292.11; 0.41

- Maximum deviation from nominal (-): 291.11; 0.59

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top | 0.006 | 0 |
| --- | --- | --- |
| 5.75” | 0.006 | 0 |
| Bottom | 0 | 0.007 |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top | 0.008 | 0.008 |
| --- | --- | --- |
| 5.75” | 0.008 | 0.008 |
| Bottom | 0.007 | 0.008 |

* 5.75” refers to 5.75” from bottom

Quality Control Technician (Print): Marva Maya Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification: 20466993 			 Hardener identification: 20488293

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1619 |  |  |  |  | 0.1619 |
| Post-Stacking (gm/point) | 0.1619 | 0.1634 | 0.1638 |  |  | 0.1631 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num | 14 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 14 |

Post-Cleanout Inspection

- Record number of Slots failing scintillator gauge block control (3.7mm):

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

- Inner Key & weld bar area clean (OK/NOK): OK		Outer Key & weld bar clean (OK/NOK): OK

Grooves clean (OK/NOK): OK				Small keys (OK/NOK): OK

Quality Control Technician (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding: February 8, 2000

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK: OK

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

- Comments:

Welder Name (Print): Cindy Dyrda Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC075 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection: July 18, 2000

- Paint batch and production date:

Batch number: 0199 20

Production Date: 14VIL1999

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 | 77 |
| Diluted paint viscosity | 22 | 15 |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm | 42.04 sec/ 6cm |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X= 20

Y= 8.5625

Z= 0.7007  42.04 seconds/ 6cm

- Visual Inspection (OK/NOK): OK

- Comments:

Mixed the paint to 15 seconds.  Started to fill the hopper at 11:25 at 40 PSI.  Inserted the submodule at 11:45 and it was totally submerged at 11:50.  Started the emptying procedures at 12:20 at 40 PSI and finished at 12:40.  The submodule was horizontal at 13:10.

Quality Control Technician (Print): Greg Wilkins Date: Signature: