ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 UNFINISHED, Weld: FULL (see page 4 for map of collapsed slots) | Institute: University of Chicago |
| --- | --- |

| ## CONTROL | ### Data | ### Comments |
| --- | --- | --- |
| #### Date of the stacking | July 7, 2000 | Drake, Brad |
| Date of final welding | July 25, 2000 |  |
| Date of surface protection | NO PAINT |  |
| Coil identification: masters | Pallet #79 |  |
| Box identification: spacers | 15-5/13 |  |
| Glue batch number | Hardener 20545093 Resin 20547093 |  |
| Glue drop size – start (gm) | 0.1538 | 14:05 |
| Glue drop size – middle (gm) | 0.1549 | 15:50 |
| Glue drop size – end (gm) | 0.1566 | 17:00 |
| Stacking time (h:m) | 2:55 |  |
| Gluing curing time ( h:m) | 3 days |  |
| Glue hardness (OK/NOK) | OK |  |
| Glue clean out (OK/NOK) |  |  |
| Tack welding: Welder name | Tracy Westmoreland |  |
| Final Welding: Welder name |  |  |
| Weld inspection (OK/NOK) |  |  |
| Observations: Spacers, Shim at inner radius of 0.003”, shim on top of 0.030” |  |  |

Last date of stacking fixture qualification	: N/A

Last date of glue system qualification 		: 12-99

Last date of welder qualification (final weld)	:

Quality Control Leader: Kelby Anderson, Elizabeth Pod Quality Control Foreman (Print): Greg Wilkins Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 | Institute: University of Chicago |
| --- | --- |

- THICKNESS MEASUREMENTS

##### According to drawing ATLLEMS_0002

Submodule Type:			STANDARD: 		Design height  = 291.7 +0.3 –1.5mm

(Circle One)

- SPECIAL:			Design height = 306.4mm

| Point | 1 | 2 | 3 | 4 | 5 | 6 | 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.29 | 291.81 | 292.02 | 292.29 | 292.22 | 292.09 | 292.03 |

| Point | 14 | 13 | 12 | 11 | 10 | 9 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.02 | 291.59 | 291.85 | 292.05 | 291.99 | 292.04 | 291.06 |

| Point | 15 | 16 | 17 | 18 | 19 | 20 |
| --- | --- | --- | --- | --- | --- | --- |
| Height(mm) | 291.18 | 291.66 | 291.91 | 292.17 | 292.11 | 292.14 |

- Maximum deviation from nominal (+):

- Maximum deviation from nominal (-):

Quality Control Technician (Print): Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 | Institute: University of Chicago |
| --- | --- |

# Feeler Gauge Measurements

- Narrow End:

- Left Side:				Right Side:

| Top |  |  |
| --- | --- | --- |
| 5.75” |  |  |
| Bottom |  |  |

- Section 1:

- (.5” from weld area on narrow end)

- Left Side:				Right Side:

| Top |  |  |
| --- | --- | --- |
| 5.75” |  |  |
| Bottom |  |  |

* 5.75” refers to 5.75” from bottom

Observations/Drawings:

Quality Control Technician (Print): Date: Signature:

ATLAS TILECAL	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 | Institute: University of Chicago |
| --- | --- |

- SUBMODULE GLUEING, INSPECTION & CLEANOUT

Gluing

Resin identification:20547093 			 Hardener identification: 20545093

Dosage control (gm/point). (Final range to be determined from glue system qualification)

- Allowed range : 0.130 – 0.180 gm/point

Allowed range for average: 0.155 +/- 0.005gm/point

| Point | 1 | 2 | 3 | 4 | 5 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| ###### Pre-Stacking (gm/point) | 0.1538 |  |  |  |  | 0.1538 |
| Post-Stacking (gm/point) | 0.1538 | 0.1549 | 0.1566 |  |  | 0.1551 |

Pre-Cleanout Inspection

- Record number of slots in which glue squeeze out has occurred:

| Cell | I | II | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Num |  |  |  |  |  |  |  |  |  |  |  |

Collapsed  slots

- Position of Slots failing scintillator gauge block control (3.7mm): (#15 on the bottom, #1 the most top one)

| Cell | I | II 4 slots | III | IV | V | VI | VII | VIII | IX | X | XI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Index |  | 7,9,13, 15 |  |  |  |  |  |  |  |  |  |

- Inner Key & weld bar area clean (OK/NOK):		Outer Key & weld bar clean (OK/NOK):

Grooves clean (OK/NOK):					Small keys (OK/NOK):

Quality Control Technician (Print): Date: Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 | Institute: University of Chicago |
| --- | --- |

- FINAL WELDING

- Date of Welding:

- Welding Filler Rod Material: ER70S-2

- Weld Inspection (as defined in technical specification) – OK/NOK:

- 1.	Inspection commenced before weld cooled to ambient temperature

(Within 20 minutes)

- 2.	No Cracks

- 3.	Thorough fusion

- 4.	All craters filled to full cross section

- 5.	Undercut does not exceed .25mm

- 6.	No visible porosity

- 7.	Weld profile conformance

- Note any required repairs:

- Note any variances from technical specification:

Weld procedure was completed to narrow end of module as follows: 3” weld on 6” centers.  Allowed to cool until almost no warmth could be felt in the weld zone.  Repeated until weld is completed.

- Comments:

Welder Name (Print): Date: Welder Signature:

ATLAS TILECAL 	SUBMODULES QUALITY CONTROL PROTOCOL

| Submodule Label: UC111 | Institute: University of Chicago |
| --- | --- |

- SURFACE PROTECTION

- Date of Surface protection:

- Paint batch and production date:

Batch number:

Production Date:

- Control of Paint Viscosity (time in 4mm Ford or Zahr Cup)

|  | Specification (s) | Measured Viscosity (s) |
| --- | --- | --- |
| Initial paint viscosity | 66 |  |
| Diluted paint viscosity | 22 |  |

- Control of Paint Flow

- Energy velocity, as specified in general QC procedures note.

- Acceptable range is 60-120s per 6cm of emerging length.

|  | Top | Middle | Bottom |
| --- | --- | --- | --- |
| Time/6cm |  |  |  |

Calculations:

171.25cm /X minutes  Ycm/1 minutes

Ycm/1 minutes = 6cm/Z minutes  6cm/Z minutes

X=

Y=

Z=

- Visual Inspection (OK/NOK):

- Comments:

Quality Control Technician (Print): Date: Signature: