## Slide 1: Progress in developing large-area high resolution photo-detectors (LAPPD)
Henry Frisch
Enrico Fermi Institute, Univ. of Chicago
and HEPD, Argonne National Laboratory

## Slide 2: The 4 `Divisions’ of LAPPD
CV
CV
Hermetic Packaging
CV
CV
Electronics/Integration
MicroChannel Plates
Photocathodes
See (hear) Eric Oberla’s talk
See (hear) Klaus Attenkofer’s talk

## Slide 3: The Large-Area Psec Photo-Detector Collaboration

## Slide 4: Parallel Efforts on Specific Applications
.
LAPD Detector Development
PET
(UC/BSD, UCB, Lyon)
Collider
(UC, ANL,Saclay.
Mass Spec
Andy Davis, Mike Pellin, Eric Oberla
Non-proliferation
LLNL,ANL,UC
Drawing Not To Scale (!)
ANL,Arradiance,Chicago,Fermilab, Hawaii,Muons,Inc,SLAC,SSL/UCB, UIUC, Wash. U
Explicit strategy for staying on task-
Multiple parallel cooperative efforts
All these need work- naturally tend to lag the reality of the detector development
Neutrinos
(Matt, Mayly, Bob, John, ..; Zelimir)
Muon Cooling
Muons,Inc
(SBIR)
K->pnn
JPARC
ANT11 audience

## Slide 5: Microchannel Plates-1
Incom Glass Substrates- Hard (untreated) glass
0.077” Multi
20-micron pores
mm Disc
(Development)
8”-square (the `Tile’)
Micro-photograph of the pore/multi structure
2 working formats:

## Slide 6: Microchannel Plates-2
Argonne ALD and test Facilities
In situ measurements of R (Anil)
Femto-second laser time/position measurements (Matt, Bernhard, Razib, Sasha)
33 mm development program
8” anode injection measurements
Anil Mani and Bob Wagner

## Slide 7: Microchannel Plates-3
SSL (Berkeley) Test/Fab Facilities
Ossy Siegmund, Jason McPhate, Sharon Jelenski, and Anton Tremsin-
Decades of experience
(some of us have decades of inexperience?)

## Slide 8: Microchannel Plates-4a
Performance: First, the gain. We see gains > 107 in a chevron-pair;
> 105 in a single plate (attractive possibility for cost/simplicity)
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB

## Slide 9: Microchannel Plates-4b
Noise (bkgd rate).
<=0.1 counts/cm2/sec; factors of few > cosmics (!)
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB
Performance:

## Slide 10: Microchannel Plates-4c
Performance: Image quality, spatial resolution, uniformity:
Good uniformity; can resolve the multi boundaries in top plate (20microns)
Ossy Siegmund, Jason McPhate, Sharon Jelinsky, SSL/UCB

## Slide 11: Microchannel Plates-4d
Performance: burn-in (aka `scrub’)
Measurements by
Ossy Siegmund,
Jason McPhate,
Sharon Jelinsky, SSL/UCB
Typical MCP behavior- long scrub-times
Measured ANL ALD-MCP behavior
(ALD by Anil Mane, Jeff Elam, ANL)

## Slide 12: First Pulses From an 8” MCP (!)
Matt Wetstein, Bernhard Adams, Razib Obaid, Sasha Vostrikov (ANL and UC)
Pulses from the 2 ends of an 8” anode strip
Caveats- this is the first time…
TDIITDs- don’t over analyze this

## Slide 13: First Pulses From an 8” MCP
Matt Wetstein, Bernhard Adams, Razib Obaid, Sasha Vostrikov (ANL and UC)
From the time difference of the 2 ends of the strip one gets the longitudinal position, from the average of the 2 ends the time (and of course from which strip(s) one gets the transverse position) => so have 2D at wall plus Time-of-Arrival
TOA (psec)
Position of laser (mm)
TrueError bar prob.
like this
(ask Matt)
Note
c= 0.3mm/ps
1/c=3.3 psec/mm

## Slide 14: MCP Prognosis
Incom has made great strides in making substrates- the 3-pt joint of the multis seems solved; some cleaning issues remain and are being worked on
Strong UHV test facilities have been constructed at SSL and ANL (this was a big effort- UHV isn’t fast or easy- requires real infrastructure)
ALD development has a 1st-generation baseline that shows high gain, low noise, and short burn-in (ALD: Anil Mane and Jeff Elam, ANL)
Transferring knowledge gained from hundreds of 33mm plates to 8” plates and Beneq machine now (Anil Mane and Jeff Elam, ANL)
Fast turn-around electroding has turned out to be an issue- we have attacked now on parallel fronts (this was a surprise)
We have started a program with Incom to produce more blocks to get enough 8” plates for a first-round of users in the field (see slide 4 for the customers)

## Slide 15: Photocathodes Subject of next talk by Klaus- touch on here only briefly
LAPPD goal- 20-25% QE, 8”-square
2 parallel efforts: SSL (knows how), and ANL (learning)
ANL
Optical stand
First cathodes made at ANL
Burle commercial
equipment

## Slide 16: Photocathodes- 2 Subject of next talk by Klaus
SSL has years of experience making bialkali photocathodes-
They are our treasury bonds (Swiss francs?) in the LAPPD `portfolio of risk’

## Slide 17: Photocathodes
But longer-term, we have started a broadly collaborative program outside of LAPPD on high QE (goal: > 50% QE) cathodes and tuning spectral response (LDRD funds now- ideal flagship for a (the) Natl. Detector Center
Hamamatsu
bialkalis
Ultra (UBA)-40%@400nb
Super(SBA)-34%@400nb
Conv. BA-25%@400nb
Note shift in peak
QE from conventional
BA to SBA and UBA
Q

## Slide 18: Photocathodes
An obvious question to this audience is:
Q
What are the economics of QE vs PMT area at constant bang-for-buck in a) CPV, and b) proton?
For example, going from 25%QE to 50%QE would allow going from a 7” tube to a 5” tube at constant photons*
Alzo, a Winston cone for a 5” tube is easier and smaller than one for a 7” tube (tho not for a wavelength-shifting plate?)
* Note `constant photons ‘doesn’t apply to time-position-sensitive detectors like LAPPD
Crudely, put, “what’s QE worth to you in $?”

## Slide 19: Electronics and Integration Subject of next talk by Eric - touch on here only briefly
20 GS/scope
4-channels (142K$)
17 GS/PSEC-4 chip
6-channels ($130 ?!)
Real digitized traces from anode

## Slide 20: Hermetic Packaging
Have moved to a tile/tray design: tray has all the electronics; only connections to tiles are HV and ground
Tiles are glued with spray glue to tray
HV divider chain is made with ALD
No pins through glass
Tile is plate glass
Anode strips connect
Modular; simple
Top seal is cold (ANL)
Hot (SSL)

## Slide 21: Hermetic Packaging
ANL/UC Glass Package
Glass package showing ALD-coated 8” MCP, grid spacer, bottom seal
(apologies for blurriness)

## Slide 22: Hermetic Packaging
SSL Ceramic Package (2 parallel paths)

## Slide 23: Hermetic Packaging
Bottom seal by Joe Gregar, ANL master glass-blower with help from Michael Minot (Minotech, Incom) and Ferro Corp
We have solved sealing over the anode strips

## Slide 24: Hermetic Packaging
Top Seal and Photocathode- this year’s priority
Commercial RFI for 100 tiles
(Have had one proposal for 7K- 21K tiles/yr)
Tile Development Facility at ANL
Production Facility at SSL/UCB
3 parallel paths

## Slide 25: Some Neutrino specific aspects
The ALICE TPC:
Drift electrons onto wires that measure where and when for each electron.
We drift photons-good time resolution would buy nothing if one integrated over a whole (blue) TPC sector- ie didn’t correlate when and where
when and where
Same holds with water cherenkov-see matt’s talk

## Slide 26: Daniel Boone
Proposal (LDRD) to build a little proto-type to test photon-TPC ideas and as a simulation testbed
`Book-on-end’ geometry- long, higher than wide
Close to 100% coverage so bigger Fid/Tot volume
Dx, Dy << 1 cm
Dt < 100 psec
Idea: to reconstruct vertices, tracks, events as in a TPC (or, as in LiA).
n
2 m
2 m
1 m
See Matt’s talk tomorrow

## Slide 27: The End
Pulses from the 2 ends of an 8” anode strip

## Slide 28: Backup slides